## Slide 1
SUMMER INTERNSHIP PROJECT 2026
Overview and Process Optimization of Bar and Rod Mill
Bhilai Steel Plant, SAIL
Internship period: 22 June 2026 to 18 July 2026
PRESENTED BY
Anshika Pandey , 23120016 Naval Deshpande, 23120053 Ojas Pandey, 23120059 Chirag Singhal, 23120031 Om Agrawal, 23120060 Priyansh Agrawal, 23120073 Siddharth Jha, 23120095
DEPARTMENT
Metallurgical and Materials Engineering, NIT Raipur
GUIDE
Mr. Shikhar Tiwary, General Manager, BRM

## Slide 2
AGENDA
Contents
Bar & Rod Mill | Bhilai Steel Plant, SAIL
2
01
Introduction: SAIL and Bhilai Steel Plant
02
Billet handling and charging
03
Reheating furnace
04
Rolling process
05
Finishing operations and process flow
06
Process optimization: objectives
07
Optimizing production processes
08
Advanced technologies and future scope
09
Conclusion

## Slide 3
INTRODUCTION
About SAIL and Bhilai Steel Plant
Bar & Rod Mill | Bhilai Steel Plant, SAIL
3
SAIL is one of India’s largest state-owned steel makers, running several integrated steel plants.
BSP lies about 40 km west of Raipur, Chhattisgarh. Set up in 1955, production began in 1959 with Soviet collaboration.
The MODEX programme added Blast Furnace 8 (Mahamaya), SMS-III, the Universal Rail Mill and the Bar & Rod Mill.
ISO 9001, ISO 14001 and ISO 50001:2018 certified; eleven-time winner of the PM’s Trophy for best integrated steel plant.
India’s largest supplier of rails: 130 m single-piece rails and 260 m welded panels for Indian Railways.
7.5 MT
Hot metal per year
7 MT
Crude steel per year
6.56 MT
Saleable steel per year

## Slide 4
INTRODUCTION
Objectives, scope and products
Bar & Rod Mill | Bhilai Steel Plant, SAIL
4
What we set out to do
Map the end-to-end workflow of the Bar and Rod Mill
Study the walking beam furnace and rolling stands
Identify bottlenecks from billet handling to dispatch
Propose ways to improve yield, energy use and safety
What the mill makes (5.5 mm to 60 mm)
TMT rebar, coil and straight, for construction
Wire rods in coil, for wire drawing and fencing
Quality bars in straight lengths, for structural and mechanical use
Special grades: spring, bearing, free-cutting, low-alloy and welding steels

## Slide 5
CHAPTER 2
Billet handling and charging
Bar & Rod Mill | Bhilai Steel Plant, SAIL
5
1
SMS-III Billets (about 2 t each) arrive after casting
2
Stockyard Buffer storage with Pole-1 and Pole-2 lines; one runs, one on standby
3
EM crane Lifts 5 to 6 billets at a time onto the charging platform
4
Hydraulic charger Separates and aligns one billet at a time
5
Roller table Sensor-controlled movement toward the furnace
Automation plus human eyes
A control room on the first floor near Pole-1 lets operators spot bent billets, scratches and damaged corners that sensors miss. If a defect is found, the whole batch goes back to the stockyard for segregation.

## Slide 6
CHAPTER 3
Reheating furnace
Bar & Rod Mill | Bhilai Steel Plant, SAIL
6
Cold billets are too strong to roll, so they are heated until the steel turns ductile and plastic.
A walking beam furnace is used: the movable beam lifts the billet about 200 mm, moves it 250 mm forward and sets it on the next fixed skid.
No dragging on the hearth, so less surface damage and fewer skid marks than a pusher furnace.
Four zones: recuperative (preheating, uses waste heat), heating, reheating and soaking.
Fully digital control, synchronized with the rolling mill.
102
billets held at a time
24
burners, digitally controlled
1130°C
billet exit temperature
Too cold raises rolling force and power. Too hot causes scale and poorer steel quality.

## Slide 7
CHAPTER 4
Rolling process
Bar & Rod Mill | Bhilai Steel Plant, SAIL
7
Furnace
Descaling
Roughing
Intermediate
Finishing
How it works
High-pressure water jets remove oxide scale before the first stand.
Stands alternate between horizontal and vertical so reduction is even from all directions.
Each roll has several grooves; one is used per campaign, set by product size.
Speed and safety
A₁V₁ = A₂V₂
Steel is nearly incompressible, so as area falls the bar speeds up. It crawls near the furnace and races at the finishing end.
Cobbles (bar jumping the path) come from bad guide alignment, wrong roll gap or temperature swings. The finishing section is the most hazardous zone.

## Slide 8
CHAPTER 5
Finishing operations
Bar & Rod Mill | Bhilai Steel Plant, SAIL
8
Water cooling
Controlled spray right after the last stand sets strength and toughness (the TMT step).
Cooling bed
Walking beam moves bars one by one, so they never overlap or collide.
Sampling
An operator takes a sample before cutting for tensile, bend, hardness and surface tests.
Cutting
High-speed shear, synchronized with rolling speed, makes commercial lengths.
Bundling
Steel straps and tags carry size, grade, heat and batch number for traceability.
Dispatch
Overhead cranes load bundles onto railway wagons.
12 mm and 16 mm
bar sizes being rolled on the day of the plant visit

## Slide 9
CHAPTER 5
Overall process flow
Bar & Rod Mill | Bhilai Steel Plant, SAIL
9
Billet from SMS-III
Stockyard
EM crane
Hydraulic charger
Roller table
Inspection
Walking beam furnace
Descaling
Roughing mill
Intermediate mill
Finishing mill
Water cooling
Cooling bed
Sampling and testing
Cutting
Bundling
Rail dispatch
Read left to right, row by row. The line is highly integrated: sensors, hydraulics and PLCs keep each stage in step, with people checking what machines cannot.

## Slide 10
CHAPTER 6
Why optimize the Bar and Rod Mill?
Bar & Rod Mill | Bhilai Steel Plant, SAIL
10
Optimization is continuous: find losses at every stage and fix them, so output rises without building new capacity.
Productivity
Higher output and fewer stoppages
Yield
Cut scale, crop, cobble and reject losses
Energy
Better furnace efficiency, waste heat recovery
Reliability
Predict failures before they happen
Quality
Tight dimensions and consistent properties
KPIs tracked: Overall Equipment Effectiveness (OEE), rolling yield, specific energy consumption.

## Slide 11
CHAPTER 7
Optimizing billets and the furnace
Bar & Rod Mill | Bhilai Steel Plant, SAIL
11
Raw material and charging
Check size, surface, grade and heat number before charging
UT, magnetic particle and laser checks catch hidden defects
FIFO, barcode and RFID tracking prevent grade mix-ups
Grade-wise storage avoids rust and handling damage
Reheating furnace
Aim for uniform temperature (about 1100 to 1250°C by grade)
PLC control of fuel, air-fuel ratio and residence time
Regenerative burners, insulation and waste heat recovery cut fuel use
Correct atmosphere and no overheating reduce scale loss

## Slide 12
CHAPTER 7
Rolling mill, yield and defects
Bar & Rod Mill | Bhilai Steel Plant, SAIL
12
Rolling mill
PLC/SCADA drives keep stand speeds in step; loopers hold tension
Computer-aided roll pass design balances reduction per pass
Automatic Gauge Control adjusts roll gap from laser measurements
Cameras and SPC catch surface and size defects online
Rolling yield
Yield (%) = finished product / billets charged × 100
Example: 96 t out of 100 t charged = 96%
Losses: scale, crop ends, cobbles, rejects
Raising yield from 95.5% to 96.2% on a 900,000 t mill gives thousands of extra saleable tonnes with no extra billets

## Slide 13
CHAPTER 8
Advanced technologies and future scope
Bar & Rod Mill | Bhilai Steel Plant, SAIL
13
01
Predictive maintenance
Sensors track vibration, temperature, oil condition and motor current. AI flags faults early so repairs fit planned shutdowns, lifting OEE.
02
Lean manufacturing
Remove waste with 5S, Kaizen and Total Productive Maintenance. Cut waiting, rework, extra inventory and needless movement.
03
Industry 4.0
IIoT sensors feed real-time data to AI models. Digital twins let engineers test changes virtually before touching the plant.

## Slide 14
CHAPTER 9
Conclusion
Bar & Rod Mill | Bhilai Steel Plant, SAIL
14
The BRM turns 2-tonne billets into bars and rods through a tightly automated chain: charging, reheating, rolling, cooling, cutting and dispatch.
The biggest gains lie in billet quality, furnace control, roll synchronization and cobble prevention, all of which feed rolling yield.
PLC, SCADA, AGC and IIoT give real-time control; predictive maintenance and AI improve reliability.
Lean practices (5S, Kaizen, TPM) keep improvement continuous.
Combining sound metallurgical practice with digital tools will keep BSP competitive on cost, quality and sustainability.

## Slide 15
Thank you
Questions are welcome.
Priyansh Agrawal | Roll No. 23120073 | Metallurgical and Materials Engineering, NIT Raipur
With thanks to Mr. Shikhar Tiwary and the BRM team, Bhilai Steel Plant